## Slide 1
Zoi-Lina Koutsogianni, Dimitrios Bikiaris, Konstantinos Triantafyllidis
Synthesis of Bio-Based Thermosetting Resins for Advanced Composite Applications in Plating on Plastics (PoP) Processes
24TH APRIL 2025
ALBUFEIRA, PORTUGAL

## Slide 2: Overview
Introduction to bio-based resins
FreeMe Project
Experimental Part & Results
Conclusions
FreeMe workshop, 24/04/2025

## Slide 3: Bio-based resins
Crude oil
FreeMe workshop, 24/04/2025
Oil refinery
Monomer production
Polymer production
Biomass
Bio-refinery
Monomer production
Polymer production
Plastic products
While the chemical structure of the resulting products may be identical, the environmental impact, carbon footprint, and resource circularity differ significantly

## Slide 4: Bio-based resins
(Ilyas & Sapuan, 2019)
FreeMe workshop, 24/04/2025
Not all bio-based plastics are biodegradable, and not all biodegradable plastics are bio-based.

## Slide 5: Bio-based resins
Thermoplastic
Thermoset
Weak intermolecular forces between polymer chains
No cross-links between chains
Softens when heated
Strong covalent bonds between polymer chains
Remains hard when heated
Epoxy resins: one of the main categories of polymeric materials used for the preparation of composite materials.
Highly reactive thermosetting polymers and pre-polymers
Characteristic epoxy group in their structure.
The more epoxy groups in their structure the higher the reactivity.
Mechanical properties
Excellent stability
Chemical resistance
Flame retardants
Flexibility in design
Properties
Applications
Coatings
Adhesives
Manufacturing
Aerospace and automotive industry
Sports equipment

## Slide 6: Bio-based resins
Over 90% of these epoxy materials are based on bis(4-hydroxyphenylene)-2,2-propane, known as bisphenol A (BPA).
BPA has been classified as carcinogen mutagen and reprotoxic (CMR), and is recognized as an endocrine disruptor. Consequently, many governments have recently hardened the legislation regarding the production and use of BPA, especially in baby’s bottles, food containers and medical supplies.
Growing environmental and economic concerns as well as the depletion of petrochemical resources has caused a rapid increase in the research and development of bio-based epoxy resins in recent years.
Bisphenol A
DGEBA oligomer
FreeMe workshop, 24/04/2025

## Slide 7: Bio-based resins
Vegetable oils
Chemical composition
Triglycerides 95-98 % (saturated fatty acids, mono- & poly- unsaturated fatty acids)
Other components 2-5 % (free fatty acids, tocopherols, polysterols, squalene, carotenoids, plenolics)
linseed oil
epoxidized linseed oil
FreeMe workshop, 24/04/2025

## Slide 8: Bio-based resins
Structure of lignocellulosic biomass and its biopolymers; cellulose, hemicellulose, and lignin.
(Source: Hernández-Beltrán, J.U. et al, Appl. Sci. 2019, 9, 3721)
Cellulose
Hemicellulose
Lignin
general formula (C6H10O5)n
30-50 %
Average MW 300000-500000
general formula(C5H8O4)n
20-40%
composed of various sugar monomers including glucose, galactose, mannose, xylose, arabinose, 4-O-methyl glucuronic acid, and galacturonic acid residues
15-25%
a random, amorphous, three-dimensional polymeric network
The main precursors of lignin.
Lignocellulosic biomass

## Slide 9: Bio-based resins
Cellulose, hemicellulose & lignin derived monomers/oligomers
Isosorbide
D-sorbitol
5-HMF
Vanillin
Essential oils (cinnamon, basil)
Eugenol
Cashew nut shell liquid
Cardanol
guaiacol
catechol
furfural
furfuryl alcohol
2-methoxy-4-propylphenol
lignin
FreeMe workshop, 24/04/2025

## Slide 10: The FreeMe Project
Sugar-derived monomers, which are low-cost and abundant, have also gained attention for epoxy prepolymer synthesis.
In this work, we have developed isosorbide and itaconic acid-based epoxy resins, and studied their properties, aiming to high biobased polymers.
Biomass
Cellulose
Hemicellulose
Lignin
C6 sugars
C5 & C6 sugars
Phenolics
Isosorbide
Itaconic acid
Hydrogenation/Dehydration
Feedstock for bio-based epoxy resins
Fermentation
Glucose
€
FreeMe workshop, 24/04/2025

## Slide 11: The FreeMe Project
FreeMe workshop, 24/04/2025
Isosorbide
Itaconic acid
Glycidylation
Glycidylation & Acrylation
Composite formulation
with Ni-salts
Application of coating on plastic substrate (ABS)
Reduction to Ni nuclei
and metallization
Resin/NiCl2

## Slide 12: Results
FreeMe workshop, 24/04/2025
Isosorbide
Epichlorohydrin
+
NaOH(aq)
T
Diglycidyl ether of isosorbide
Itaconic acid
Epichlorohydrin
+
NaOH(aq)
Catalyst, T
Diglycidyl ether of itaconic acid

## Slide 13: Results
FreeMe workshop, 24/04/2025
ABS substrates
Coated with bar-type applicator
DGEBA
Coating thickness ~ 50 μm
Isosorbide based
Itaconic acid based
0%
1%
Composites with NiCl2 coated on ABS
0%
0.5%
0%
1%
0.5%
1%
0.5%

## Slide 14: Results
DGEBA
Isosorbide based
Itaconic acid based
1%
1%
1%
Reduction with NaBH4
SEM
ABS
DGEBA
ITE
ISE
1% NiCl2
1% NiCl2 -reduced
1% NiCl2
1% NiCl2 -reduced
1% NiCl2
1% NiCl2 -reduced
FreeMe workshop, 24/04/2025

## Slide 15: Results
Samples reduced and treated in Electroless Ni-P bath
DGEBA + 0.1% Ni
ISE + 0.1% Ni
ITE + 0.1% Ni

## Slide 16: Conclusions
We successfully synthesized and characterized bio-based thermosetting resins from isosorbide and itaconic acid.
All systems — including bio-based ones — enable nickel salt incorporation and successful reduction. The NaBH₄ treatment leads to visible metallization in all cases.
These resins demonstrated effective metallization properties when applied to ABS substrates, making them suitable for plating on plastics applications.
Our work contributes to the ongoing effort of replacing hazardous BPA with sustainable, bio-based alternatives, without sacrificing performance.
FreeMe workshop, 24/04/2025

## Slide 17
NAME: Zoi-Lina Koutsogianni
EMAIL: koutsogiannizl@gmail.com
FreeMe workshop, 24/04/2025