## Slide 1
EXELISIS
Kostas Pyrgakis
Surfaces, Interfaces & Coatings Technologies
International Conference
24 April 2025
Albufeira, Portugal
A process optimization tool for emerging Plating on Plastics Processes

## Slide 2: CONTENTS
Etching technology introduction
Models development
Example

## Slide 3
Plating on Plastics (PoP)
Plastics: low density, lightweight, low cost
Metal coating:
  Protection: wear resistance and corrosion
  shiny, polished, aesthetic
Plastic before/after plating
Plating baths
Everyday examples

## Slide 4
Plastics Etching Technology
Technology by

## Slide 5
Etching with Cr6+
  50-70 oC – high risk environment
  Carcinogenic and highly toxic
Activation with Pd
  Critical Raw material
Plating on Plastics (PoP)
Conventional Approach
Etching
with Cr6+
Activation-Reduction
with Pd
& Sn
Plating
SSbD PoP
Non-toxic & environment
REACH compliant
Abundancy
Indispensable Need for:
Technology by

## Slide 6
Etching
with Cr6+
Activation-Reduction
with Pd
& Sn
Plating
Plating on Plastics (PoP)
Conventional Approach
Etching
with
Activation
with
Reduction
Plating
Piranha Solution
(H2O2-H2SO4)
Ni Salts
Novel
Technology
NaBH4
Technology by

## Slide 7
Cleavage of double bonds
Hydrophilic groups (-COOH, -OH)
Further activation with metal ions
micro-/nano-sized cavities
surface area ↑
Etching with Piranha (H2O2-H2SO4)
HO
OH
ABS
butadiene
Performance
Hydrophilicity
Contact Angle
Etching
Technology by

## Slide 8
Activation with Ni Salts
C – C – C – C – C – C – C – C – C – C
Etched plastic surface
Ni2+
O
O
OH
OH
OH
[NiA]
[HA]
[NiA]
Chemical adsorption
Initial metal nucleation sites
Chemical identity of metalization precursor (not binding)
Uniform distribution
Homogeneous growth
Hydrophilic groups (-COOH, -OH)
Technology by

## Slide 9
Etched plastic surface
C – C – C – C – C – C – C – C – C – C
Ni2+
O
O
Ni2+
O
O
Ni2+
O
O
Reduction
Etched plastic surface
C – C – C – C – C – C – C – C – C – C
Ni0
O
O
Ni0
O
O
Ni0
O
O
BH4-
Na+
BH4-
Na+
BH4-
Na+
e-
e-
Reduction to metallic state (MX+  M0)
Nucleation sites for metal coating (electroless step)
Strong reducing agent (NaBH4, KBH4)
NaBH4 – reducing power & low price
Technology by

## Slide 10
Platting
Step-1: NiP electroless plating
5 μm
NiP coating
𝑁𝑖2++𝐻2𝑃𝑂2−+𝛨2𝛰→𝑁𝑖0+ 𝐻2𝑃𝑂3−+ 2𝐻+
𝐻2𝑃𝑂2−+𝐻2→𝑃 (𝑠)+ 𝛨2𝛰+𝑂𝐻−
5+ μm
Ni coating
Step-2: Ni Electroplating
Anode: 𝑁𝑖0 ‒ e− → 𝑁𝑖2+
Cathode (item): 𝑁𝑖2+ + e− → 𝑁𝑖0
Technology by

## Slide 11
Modeling Etching Technology
Decision Support Tools
From Lab to Computer
Technology by

## Slide 12
User-defined
Items characteristics
Specifications
Inputs
Decision Support Tool (DST)
Etching Technology
Automotive
equipment
3 MPa
DST
Property models
Unit operation models
Process Optimization
  Concentrations
  Dilution rates
  Operating times
  Volumes
  Operating conditions
  Achieved Specifications
  Outputs

## Slide 13
Fed with:
Decision Support Tool – Background
f (x1,x2,x3,…,xN)
g (x1,x2,x3,…,xN)
Experiments database
Conditions per Stage
Specifications (Contact Angel, Adhesion, Thickness)
Mass Balances
Kinetics
Electrochemistry
Unconventional data
Combinatorial insights
Operating conditions  Outputs
State of the Art Models
Regression Models

## Slide 14: Etching stage
Assumptions
1:4 H2O2:H2SO4  > stoichiometry
>14 H2O2 molecules/monomer
Monomer-by-monomer ceasing
SEM & Optical microscope
Surface characteristics
Holes & Diameter ranges
Scaling etchning performance - [H2O2] ↑
  D ↑
  Number of holes ↓↓
[H2O2-H2SO4]

## Slide 15: Contact Angle property model
Time
Cont. Angle
Initial plastic substrate
Initiating etching
Intensive etching
Smoothed surface
Gradual cavities creation

## Slide 16: Contact Angle property model
Contact Angle estimation model
A=Boundary conditions
C, D, E =0
Rules
at
There is a pattern

## Slide 17: Contact Angle property model
Modified DIPPR Equation #115
Parameter estimation model
Rules
Optimal Concentration →

## Slide 18: Activation stage
1 (before)  2 (after) activation
[OH] vs Cont Ang
– C – C –
Ni2+
O
O
[NiA2]
[HA]
[HA]
Equilibrium
[OH] Calculation= f (CA)
[OH] Before/After Activation

## Slide 19: Reduction stage
BH4-
Na+
2∙e-
– C – C –
Ni2+
O
O
– C – C –
Ni0
O
O
BH4-
Na+
Ni2+ + 2 ∙ BH4−​ + 6∙H2​O → Ni0 + 2 ∙ B(OH)3​ + 7H2​
Ni2+ + BH4−​ → NiB + H2​ + byproducts
Reduction reaction
Undesired parallel reaction - [NaBH4] ↑↑↑
Experiments
R2=0,9626
Kinetic model fitting

## Slide 20: Plating stage
Plastic substrate
Electroplating
Δh [μm]
Adhesion
Fixed NiP Recipe
5 μm
Combined contribution | Contribution
Combined contribution | Contribution

## Slide 21: Plating stage
Plastic substrate
Electroplating
Δh [μm]
Adhesion
Fixed NiP Recipe
5 μm
Combined contribution | Contribution
Combined contribution | Contribution
R2=0,8539

## Slide 22: Technology Simulation Model
Subject to
Optimize [Objective] = Safe & Sustainable by Design
SSbD (weighted)
w1
w2
w3
Economic
Environmental
Safety
on/off
on/off
on/off
User Options
Economic
Environmental
Safety
i.e. , ,
Economic
Environmental
Safety
Indicators

## Slide 23: Decision Support Tool
User selects type of Objective
to optimize the design
Parameters & Variables
Equations system
Background code  VBA
  Optimization problem
  Interface with users
Web Platform
Available Online
Free period for Demo

## Slide 24: Example
Inputs set by USER | 
Number of Items | 100
Item surface | 20 cm2 (2 x 10 x 1 cm)
Thickness Specification | 10 μm
Adhesion Specification | 2,5 MPa
Automotive equipment
Adhesion [Mpa]
Dilution (Piranha-Water)
Piranha (H2O2-H2SO4)
Etching time [sec]
Reduction: NaBH4 [gr/lt]
Activation: NiA [gr/lt]
Reduction time [sec]
Plating time [hr]
Plating: I density [A/dm2]
Thickness [μm]
1:0,5
1:7,1
21
Econom
10
9,7
300
2
1,54
10
2,55
Volume (lt)
25
1:1,5
1:4
120
Envir/Safety
10
10
300
2
6
24,4
2,55
25
1:1,4
1:4
120
SSbD
10
10
300
2
1,54
10
2,55
33%-33%-33%
1:2,1

## Slide 25: Example
Inputs set by USER | 
Etching bath | 400 lt
Reduction bath | 400 lt
Number of Items | 10,000
Item surface | 20 cm2 (2 x 10 x 1 cm)
Thickness Specification | 14 μm
Adhesion Specification | 2,5 MPa
Automotive equipment
Adhesion [Mpa]
Dilution (Piranha-Water)
Piranha (H2O2-H2SO4)
Etching time [sec]
Reduction: NaBH4 [gr/lt]
Activation: NiA [gr/lt]
Reduction time [sec]
Plating time [hr]
Plating: I density [A/dm2]
Thickness [μm]
1:1
1:6,9
15
Econom
24,2
10
300
1,90
0,15
14
2,55
1:2,1
1:4
120
Envir/Safety
24,2
10
300
2
0,15
14,6
2,55
1:2,1
1:4
15
SSbD
24,2
10
300
1,94
0,15
14
2,55
33%-33%-33%
FreeMe Decision Support Tool
Solution <1 sec
High throughput analysis
Integrated with Real-time monitoring
Live process optimization & management
Everyday planning

## Slide 26
NAME: Kostas Pyrgakis, EXELISIS
EMAIL: kostas.p@exelisis.gr