## Slide 1
IDENER
FRANCISCO DANIEL GARCÍA ROMERO
FreeMe
A Multiscale Model for the Etching Mechanism of a Piranha Solution
on an ABS Substrate

## Slide 2
Motivation and context
Traditional metallisation techniques rely on hazardous substances (e.g. Cr⁶⁺, Pd)
Safer and greener alternatives are urgently needed in polymer surface treatment
Piranha solutions (H₂SO₄ + H₂O₂) offer a metal-free oxidative method to increase surface energy.
Understanding their interactions at molecular level can accelerate their development

## Slide 3
Objective & multiscale approach
DFT → Reaction mechanism at the molecular level
MD → Dynamic interaction with ABS surface
kMC → Surface oxidation over time

## Slide 4
DFT modelling
ABS reactions studied
Reaction 1: Oxidation of Acrylonitrile
Reaction 2: Oxidation of Butadiene
Reaction 3: Electrophilic sulfonation of Styrene
Elementary reaction steps were simulated with NWChem to obtain activation energies and rate constants.

## Slide 5
DFT: Reaction mechanism of acrylonitrile
Piranha solution
A1. Protonation
A2. Nucleophilic attack by water

## Slide 6
DFT: Reaction mechanism of acrylonitrile
Piranha solution
A3. Proton transfer
A4. Resonance

## Slide 7
DFT: Reaction mechanism of acrylonitrile
Piranha solution
A5. Deprotonation

## Slide 8
DFT: General procedure
Procedure applied to all reaction steps
Geometry optimisation of reactants and products
Vibrational frequency analysis to confirm stability
Transition state search from both sides
Validation via single imaginary frequency
Energy of activation calculated for each step
Computational details
Software: NWChem (run via WebMO)
Basis set: initially 6-31++G**, later replaced by 6-31G*
Reason: 6-31G* provided comparable activation energies with faster convergence
Gibbs Free Energy approximated by DFT energy (enthalpy and entropy corrections negligible)

## Slide 9
DFT: Reaction mechanism of butadiene
Piranha solution
B1.
B2.

## Slide 10
DFT: Reaction mechanism of butadiene
Piranha solution
B3.
B4.

## Slide 11
DFT: Reaction mechanism of butadiene
Chart: DFT energy
| 5 | 6
 | -384.5458 | -384.5458
 | -384.5458 | -384.5334
 | -384.5334 | -384.5334
 | -384.5334 | -384.6205
 | -384.6205 | -384.6205
 | -384.6205 | -384.6198
 | -384.6198 | -384.6198
 | -384.6198 | -384.6459
 | -384.6459 | -384.6459
 | -384.6459 | -384.6415
 | -384.6415 | -384.6415
 | -384.6415 | -384.6482
B2R
B2P/B3R
B2T
B3T
B3P/B4R
B4T
B4P

## Slide 12
DFT: Reaction mechanism of butadiene
Piranha solution
C1.
C2.

## Slide 13
DFT: Reaction mechanism of styrene
P1.
P2.

## Slide 14
Molecular dynamics: Overview
ABS block built from 70 monomers using OPLS
Reactive etching simulated using ReaxFF
“Molecular gun” approach used to simulate impact
Different H₂SO₄:H₂O₂ ratios and energies tested
Analysis: MSD, diffusion, penetration, mass loss, species evolution

## Slide 15
The method used to introduce the piranha solution molecules is based on adding them at the top surface of the simulation box, with randomly selected (x,y)-coordinates and a constant incident energy, with an established time between insertions.
Different concentrations were considered: 4:1, 5:1, 7:1, 10:1; with around 55-60 total piranha solution molecules introduced for each case. And different insertion energies are tested.
After all molecules are inserted, the simulation keeps running to analyse the etching process.
Etching time evolution
Excessive energy case

## Slide 16
Molecular dynamics: MSD and diffusion
0.4 eV

## Slide 17
Molecular dynamics: MSD and diffusion
0.6 eV

## Slide 18
Molecular dynamics: MSD and diffusion
0.8 eV

## Slide 19
Molecular dynamics: MSD and diffusion

## Slide 20
Molecular dynamics: Penetration depth

## Slide 21
Molecular dynamics: Penetration depth

## Slide 22
Molecular dynamics: Species analysis

## Slide 23
Monomer distribution
Rate calculation
Random event takes place
Update surface
Repeat process
Kinetic Monte Carlo

## Slide 24
Kinetic Monte Carlo

## Slide 25
PRESENTER: Francisco Daniel García Romero (francisco.garcia@idener.ai)
TEAM: Israel Bellanato (israel.bellanato@idener.ai); Andrea Martos (andrea.dominguez@idener.ai); Albert Sabadell (albert.sabadell@idener.ai)